## Slide 1
KVX Wear Bar
An excellent Sagitta steel wear protection solution for a wide range of applications including:
Bucket liners (internal & external, in both impact and wear zones)
Dozer blade liners (some applications)
Hopper liners (crushers, feeders, etc)
Dump truck liners (long wearing & easy to replace quickly where worn)
Features/benefits:
~500HB throughout
High KVX toughness
No stripping defects
No stripping losses
No stripping labour
Attractive economics!
Typical customer comment:
“As easy to weld as 400HB, and wears longer than competitive 500HB!”

## Slide 2
KVX Wear Bar

## Slide 3
KVX Wear Bar

## Slide 4
Application: 800t FS x 3 (Gold Mine, Australia)
Replace troublesome mechanical wear caps
Protect cast lip internally
Protect cast lip externally
Protect impact zones on main bucket shell
Wear liners, underside of clam
KVX Wear Bar

## Slide 5
Customer is utilising KVX rolled “banana bars” externally on the clam (high wear and impact)
These custom rolled parts (50~60mm thick) were previously made from Hardox 450 (450 HB)
Previous results with Hardox 450: max 4,000hrs (typically 3500hrs)
KVX versions with same dimensions lasting 10~12,000hrs!
KVX Wear Bar
Application: 800t FS x 3 (Gold Mine, Australia)